# Adhesive Failure Mode Decision Chart

| Case or test reference |  |
| --- | --- |
| Joint or part description |  |
| Prepared by (name, role) |  |
| Date (YYYY-MM-DD) |  |

# Instructions

1. Use this chart for a bonded joint that failed in a mechanical test or in service, with both halves kept.

2. Fill Part 1 before you classify the joint. Keep both halves clean and dry; photograph them under the same light with a scale.

3. Run the decision steps in Part 2 on each half. Read with the naked eye first, then use magnification where step 2 asks for it.

4. Record each pattern with its ISO 10365:2022 designation, its area share (% of bonded area) and its location in Part 3.

5. Use the chart in Part 4 to list candidate causes. Each candidate cause is a hypothesis, not a conclusion.

6. Write each hypothesis, its next check, owner and result in Part 5. A hypothesis nobody checked stays open.

7. In a test report, write the ISO 10365:2022 designation after each pattern (AF, CF, SCF, SWCF, SF, CSF, DF, ACFP, COR). For more than one pattern, give an approximate percentage after each designation; add OSC for an oscillating failure, for example AF (50 %) + CF (50 %), OSC.

8. Any solvent wipe test follows the adhesive's and solvent's safety data sheets (SDS) and your site's chemical handling rules.

9. The chart does not decide whether a failure pattern is acceptable. The product specification or qualification plan does.

10. The illustrative example at the end describes an invented case. It is not data from a real product, customer or result.

# 1. Joint and failure record

| Adhesive (type, product, lot) |  |
| --- | --- |
| Adherend 1 (material, grade, thickness in mm) |  |
| Adherend 2 (material, grade, thickness in mm) |  |
| Mix ratio, two-part systems (specified; recorded) |  |
| Cure (time in min or h; temperature in °C) |  |
| Surface preparation (method, procedure revision) |  |
| Time from preparation to bonding (min or h) |  |
| Bond-line thickness (mm; designed, measured) |  |
| Test method and conditions, or service history (load type, °C, % RH, time in service, exposure) |  |
| Failure load (N or MPa) and expected value for the same test (source) |  |
| Both halves kept: [ ] yes [ ] no |  |
| Photographs taken with scale: [ ] yes [ ] no |  |
| Retained good joint or coupon available: [ ] yes [ ] no |  |

# 2. Decision steps (run on each half)

| Step | Question | If yes | If no |
| --- | --- | --- | --- |
| 1 | Is adhesive present on both fracture surfaces? | [ ] Go to step 4 | [ ] Go to step 2 |
| 2 | Under magnification, does the bare-looking surface carry a thin, continuous adhesive film? | [ ] Record thin-layer cohesive, then go to step 5 | [ ] Go to step 3 |
| 3 | Are there corrosion products at the interface, spreading from the edges? | [ ] Record bondline corrosion (COR), then go to step 5 | [ ] Record adhesive (interfacial) failure, AF, then go to step 5 |
| 4 | Is the adhesive whitened along the fracture? | [ ] Record stress whitening (SWCF), then go to step 5 | [ ] Record cohesive (CF), then go to step 5 |
| 5 | Is the adherend itself torn, delaminated or broken in any area? | [ ] Record substrate (SF) for that area, then go to step 6 | [ ] Go to step 6 |
| 6 | Does more than one pattern appear? | [ ] Record mixed, with an approximate percentage after each designation, then go to step 7 | [ ] Go to step 7 |
| 7 | Is the failure load below the expected value for the same test? | [ ] Test the low-load causes in the pattern row | [ ] Test the design-limit causes in the pattern row |

# 3. Patterns recorded

| Half (1 or 2) | Pattern | Area share (% of bonded area) | Location (edge, centre, start of peel) | Magnification used (x) |
| --- | --- | --- | --- | --- |

# 4. Chart: pattern, candidate causes and next checks

Candidate causes are hypotheses to test, not conclusions.

| Failure pattern | What both surfaces show | Candidate causes (hypotheses) | Next check |
| --- | --- | --- | --- |
| Adhesive (interfacial), AF | Adhesive on one side, bare adherend on the other | Surface contamination; low surface energy; surface preparation outside procedure; water at the interface after exposure | Surface preparation record and time to bonding; surface analysis (for example XPS) of the bare side |
| Thin-layer cohesive | Thin adhesive film left on the bare-looking side | Weak layer near the interface: primer, partial contamination, interphase cure (inference) | Magnified inspection; surface analysis of the film side |
| Cohesive in the adhesive, CF | Adhesive on both sides | At expected load: adhesive strength or joint design is the limit. At low load: under-cure, mix ratio, bond-line thickness, voids, water uptake | Failure load against expected value; cure records; degree of cure (for example DSC); dispense records; bond-line thickness |
| Stress whitening (SWCF) | Whitened adhesive along the fracture (appearance inferred; designation from ISO 10365:2022, Table 1) | Adhesive likely deformed before failing (inference); load or temperature at the edge of the design range | Load and temperature history against the joint design |
| Substrate, SF (CSF, DF) | Adherend torn, delaminated or broken (FRP: fiber-tear, light-fiber-tear, stock-break) | Bond stronger than the adherend; adherend thickness, grade or laminate surface layer; test geometry | Adherend properties; whether the test kept the adherend below yield |
| Bondline corrosion (COR) | Corrosion products at the interface, often from the edges (appearance inferred; designation from ISO 10365:2022, Table 1) | Water and salt reaching the metal interface | Exposure history; pretreatment and primer records |
| Mixed | Two or more patterns, each with an approximate percentage after its designation | Local variation in surface preparation, contamination or bond-line thickness (inference) | Map where each pattern sits; match zones to process steps |

# 5. Hypotheses to test

| ID | Candidate cause (hypothesis) | Next check (record or test) | Owner | Result: [ ] supports [ ] refutes [ ] open |
| --- | --- | --- | --- | --- |

# 6. Limits of this reading

[ ] Only one half was kept.

[ ] Surfaces were cleaned, handled or exposed after failure.

[ ] Failure load or test conditions are unknown.

[ ] A surface layer may be thinner than the analysis method can see.

| Effect of the limits on the reading |  |
| --- | --- |
| Reviewed by (name, date) |  |

# Illustrative example (invented case, not real data)

Case (illustrative): a line bonding powder-coated steel brackets to a glass-fiber reinforced polyester panel with a two-part epoxy reports low lap shear values on one shift. Five coupons failed.

| Coupon | Pattern recorded | Area share and location | Next check chosen |
| --- | --- | --- | --- |
| 1 to 3 | Adhesive (interfacial) on the steel side | 90 % of area, whole joint (illustrative) | Preparation log for that shift; time from wipe to bonding |
| 4 | Mixed: interfacial and cohesive | Interfacial 30 % at one edge, cohesive 70 % (illustrative) | Map against handling points |
| 5 | Substrate: light-fiber-tear on the panel side | Panel surface layer (illustrative) | None for the bond; note panel surface |

| ID | Candidate cause (hypothesis) | Next check | Result (illustrative) |
| --- | --- | --- | --- |
| H1 | Contamination of the coated steel before bonding | Preparation log; surface analysis of bare steel side | Open |
| H2 | Wrong mix ratio on that shift | Dispense records; metering check by weight | Open |
| H3 | Under-cure | Cure oven record; degree of cure | Open |